## Slide 1: Template of the Process flow
All user must submit a process flow and obtain approval before booking ALL equipment.
Oversimplified process flow is not accepted.
Violate the process flow and the instruction from Officer will be forbidden to enter Cleanroom for one week

## Slide 2
Process Flow of (the name of Process Flow, e.g Pattern Transfer on Si)
Si
Step No. | Equipment | Process | Requirements
1 | Wet Bench in Clean 100 | Acetone, IPA and DI water cleaning | 5 mins with ultrasonic
2 | Sawatec SM-180-BT Spin Coater | AZ5214 Photoresist coating | Photoresist thickness with 1.5 um (500 rpm 5 sec, 4000 rpm 30 sec)
3 | Sawatec HP-150 Hot plate | Pre baking | 100˚C for 1 min
4 | OAI 806 MBA | Pattern Transfer | Soft contact
5 | Wet Bench in Clean 100 | AZ400K / DI Water (1:4) developing | 1 min
6 | Wet Bench in Clean 100 | DI Water Cleaning | Dry by Compress N2
PR
Si
Cross section of the sample at the step
Process Flow No: | (NetID-Email Date-Process #; eg.20000000R-281022-01) | Name and PolyU ID no(if available) : | XXX | Sample description : | (Materials, size, number of sample….) | Date(dd-mm-yyyy): | XXX